ELEVATE-LNP: Empty Lipid Nanoparticle Enabled Validation and AI-Guided Therapeutic Evaluation for Efficient Formulation Optimization for mRNA Delivery

Mingzhi Yu1†, Luhan Wang1†, Timothy Elliott1, Xianqing Wang2, Allen Mathew1, Bei Qiu2, Liang Yao2, Wenxin Wang2, Nan Zhang1*

1. Centre of Micro/Nano Manufacturing Technology (MNMT-Dublin), School of Mechanical & Materials Engineering, University College Dublin, D04 V1W8, Ireland.

2. Charles Institute of Dermatology, School of Medicine, University College Dublin, D04 V1W8, Dublin, Ireland.

†These authors contributed equally: Mingzhi Yu, Luhan Wang.

*Corresponding author. E-mail: nan.zhang@ucd.ie

Fig. S1 Preliminary optimization of N/P ratio for GFP mRNA-loaded LNPs.

GFP mRNA-loaded LNPs were prepared at N/P ratios of 6, 8, and 10 to evaluate the influence of N/P ratio on LNP physicochemical properties and transfection performance. (a) Particle size and PDI of LNPs prepared at different N/P ratios. LNPs prepared at N/P 6 showed a larger particle size, whereas N/P 8 and N/P 10 resulted in smaller and comparable particle sizes. (b) Quantification of GFP fluorescence intensity (GFP IntDen) in cells transfected with LNPs prepared at different N/P ratios. N/P 8 produced the highest GFP signal among the tested conditions. (c) Representative fluorescence microscopy images of GFP expression after transfection with LNPs prepared at N/P ratios of 6, 8, and 10.

Fig S2. Percent error, MSE, MAE and average R2 for nested cross-validation for size

Figure S3. Accuracy, F1 score, precision and recall for nested cross-validation for PDI

Fig. S4 Spearman correlation matrix of formulation features in relation to LNP size and PDI.

Fig. S5 Experimental validation of model-selected formulations with GFP mRNA. (a) The size and PDI of 100 GFP mRNA–loaded formulations; (b) EE of the same formulations; (c) GFP fluorescence intensity (GFP intDen) in CFBE cells 48 h post-transfection; (d) Cell viability of CFBE cells after transfection with the corresponding formulations.

Fig. S6 Spearman correlation matrix of formulation features in relation to transfection efficiency.

Table. S1 Six lead formulations selected for CFTR mRNA encapsulation and Western blot validation

| No. | ILT | HLT | ILC | ILR | HLP | PLR | CR |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | SM-102 | DOPC | 0.0025 | 40 | 16 | 0.5 | 43.5 |
| 2 | SM-102 | DOPC | 0.0055 | 44 | 16 | 0.5 | 39.5 |
| 3 | SM-102 | DOPC | 0.004 | 40 | 16 | 0.5 | 43.5 |
| 4 | SM-102 | DSPC | 0.01 | 48 | 16 | 0.5 | 35.5 |
| 5 | SM-102 | DSPC | 0.01 | 52 | 16 | 0.5 | 31.5 |
| 6 | SM-102 | DSPC | 0.0085 | 48 | 16 | 0.5 | 35.5 |

Table. S2 Best parameters for different ML models of nested cross-validation for size

|  | Best Parameters | Frequency |
| --- | --- | --- |
| GPR | {'alpha': 0.1, 'kernel': '1**2 * RationalQuadratic(alpha=1, length_scale=1)', 'n_restarts_optimizer': 0, 'normalize_y': True} | 25 |
| SVR | {'C': 10, 'degree': 3, 'epsilon': 1.0, 'kernel': 'rbf'} | 61 |
| XGBR | {'colsample_bytree': 1.0, 'learning_rate': 0.01, 'max_depth': 5.0, 'min_child_weight': 4.0, 'n_estimators': 200.0, 'subsample': 0.8} | 29 |
| GBR | {'learning_rate': 0.01, 'max_depth': 3.0, 'min_samples_leaf': 4.0, 'min_samples_split': 10.0, 'n_estimators': 400.0, 'subsample': 0.8} | 18 |
| RF | {'max_depth': 5, 'min_samples_leaf': 4, 'min_samples_split': 2, 'n_estimators': 200} | 19 |
| Ridge | {'alpha': 100} | 99 |
| ANN | {'batch_size': 16.0, 'lr': 0.001, 'max_epochs': 100.0, 'module__hidden_size': 128.0} | 30 |

Table. S3 Best parameters for different ML models of nested cross-validation for PDI

|  | Best Parameters | Frequency |
| --- | --- | --- |
| GP | {"kernel": "1**2 * RBF(length_scale=1)"} | 200 |
| SVM | {"C": 0.1, "gamma": "auto", "kernel": "rbf"} | 114 |
| XGB | {"colsample_bytree": 0.8, "gamma": 0.1, "learning_rate": 0.1, "max_depth": 5.0, "min_child_weight": 5.0, "n_estimators": 200.0, "subsample": 0.8} | 18 |
| GB | {"learning_rate": 0.1, "max_depth": 3.0, "min_samples_leaf": 4.0, "min_samples_split": 2.0, "n_estimators": 200.0} | 26 |
| RF | {"max_depth": 10.0, "min_samples_leaf": 1.0, "min_samples_split": 2.0, "n_estimators": 200.0} | 32 |
| LR | {"C": 0.0001, "penalty": "l2", "solver": "lbfgs"} | 90 |

Table. S4 Best parameters for different ML models of nested cross-validation for transfection efficiency

|  | Best Parameters | Frequency |
| --- | --- | --- |
| GPR | {'alpha': 0.1, 'kernel': '1**2 * RationalQuadratic(alpha=2, length_scale=1)', 'n_restarts_optimizer': 0, 'normalize_y': True} | 51 |
| SVR | {'C': 10, 'epsilon': 0.1, 'kernel': 'rbf'} | 99 |
| XGBR | {'colsample_bytree': 0.8, 'learning_rate': 0.1, 'max_depth': 3.0, 'min_child_weight': 1.0, 'n_estimators': 100.0, 'subsample': 0.8} | 89 |
| GBR | {'learning_rate': 0.1, 'max_depth': 5.0, 'min_samples_leaf': 1.0, 'min_samples_split': 2.0, 'n_estimators': 100.0, 'subsample': 0.8} | 42 |
| RF | {'max_depth': 5, 'min_samples_leaf': 1, 'min_samples_split': 2, 'n_estimators': 50} | 30 |
| Ridge | {'alpha': 1} | 92 |